Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

#### GMAW(GAS METAL ARC WELDING)(MIG) #18 PROCEDURE: - Select proper equipment for GMAW process. - Cut one piece ¼” x 5” x 5” mild steel plate - Set machine according to chart located inside panel - Wire side is .035 - Set Argon/CO² to 25 psi - Re-adjust if necessary - Use proper welding techniques for flat position. - ONE SIDE ONLY – deposit a series of adjacent parallel beads to cover an area 4 x 4 inches. - Each bead must be overlapping ¼ to ½ way with the adjoining bead so that a continuous layer of metal is formed - Deposit a second series of parallel beads over the first layer at right angles to the first. - Deposit a third series of parallel beads over the second layer at right angles to the second. - Once completed, clean welds before presenting to instructor. - DO NOT TURN IN HOT METAL ## GMAW ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Evidence of undercuts 5 pts _______________ Evidence of porosity 8 pts _______________ Evidence of slag inclusion 3 pts ________________ Overlapping techniques 10 pts ________________ Penetration 2 pts ________________ Comment: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# BEAD PAD – E6011 & E7018 #1 & 2 PROCEDURE: - Select proper equipment for electric arc welding. - Use one side E6011 the opposite side of the E7018 pad - Set amperage setting 90-100 - Set polarity lever to DC only - Re-adjust if necessary - Use proper welding techniques for flat position. - ONE SIDE ONLY – deposit a series of adjacent parallel beads to cover an area 4 x 4 inches. - Each bead must be overlapping ¼ to ½ way with the adjoining bead so that a continuous layer of metal is formed - Chip and clean all slag thoroughly before depositing a second layer - Deposit a second series of parallel beads over the first layer at right angles to the first. - Deposit a third series of parallel beads over the second layer at right angles to the second. - Once completed, clean welds before presenting to instructor. - DO NOT TURN IN HOT METAL ## E6011 & E7018 Scorecard E6011 E7018 Follow direction: 2 pts _______¦________ Bead width 10 pts _______¦________ Uniformity of beads 10 pts _______¦________ Evidence of undercuts 5 pts _______¦________ Evidence of porosity 5 pts _______¦________ Evidence of slag inclusion 6 pts ________¦________ Overlapping techniques 10 pts _______¦_________ Penetration 2 pts _________________ Comments: Total 50 pts _______¦_________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# LAP WELD – E6011 ONLY #### FLAT ONLY #3 PROCEDURE: - Select proper equipment for electric arc welding. - Cut 2 - ¼” x 2” x 4” mild steel flat bar(use ¼ x 2” Flat bar) - Select 1/8” E 6011 electrode - Set amperage setting 90-100 and adjust accordingly - Set polarity lever to AC only. - Place the two pieces of metal so they overlap 1 inch. (protect your finished work from spatter.) - Tack weld both ends of plates. - Use a single bead one side and overlapping beads to cover the lab joint on the opposite side. - Keep the electrode at an angle of from 30 to 45 degrees with the lower plate - Hold the arc slightly longer on the lower plate. - Use proper techniques welding in flat position only. - DO NOT TURN IN HOT METAL ## E6011 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 8 pts _______________ Evidence of undercuts 8 pts _______________ Evidence of porosity 4 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 8 pts ________________ Penetration 4 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# LAP WELD – E7018 ONLY #### FLAT ONLY #4 PROCEDURE: - Select proper equipment for electric arc welding. - Cut 2 - ¼” x 2”x 4” mild steel flat bar(use ¼ x 2” Flat bar) - Select 1/8” E7018 electrodes - Set amperage setting 90-100 and adjust accordingly. - Set polarity lever to DC only - Place the two pieces of metal so they overlap ¼ to ½ inch. (protect your finished work from spatter.) - Tack weld both ends of plates. - Use a single bead pass on one side and overlapping beads to cover the lab joint on opposite side. - Keep the electrode at an angle of from 30 to 45 degrees with the lower plate - Hold the arc slightly longer on the lower plate. - Use proper techniques welding in flat position only. - DO NOT TURN IN HOT METAL ## E7018 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 8 pts _______________ Evidence of undercuts 8 pts _______________ Evidence of porosity 4 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 8 pts ________________ Penetration 4 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# TEE FILET – E6011 ONLY #### FLAT ONLY #5 PROCEDURE: - Select proper equipment for electric arc welding. - Cut 2 pieces - ¼” x 2”x 4” mild steel flat bar(use ¼ x 2” Flat bar) - Select 1/8” E 6011 electrode - Set amperage setting 90-100 and adjust accordingly. - Set polarity lever to AC only. - Set two pieces together at right angles forming a tee joint and tack weld both ends. - Make one bead pass on one side and three overlapping bead passes to complete the fillet weld on opposite side. - Use proper techniques welding in flat position only. - DO NOT TURN IN HOT METAL ## E6011 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Evidence of undercuts 5 pts _______________ Evidence of porosity 4 pts _______________ Evidence of slag inclusion 4 pts ________________ Overlapping techniques 10 pts ________________ Penetration 5 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# TEE FILLET – E7018 ONLY #### FLAT ONLY #6 PROCEDURE: - Select proper equipment for electric arc welding. - Select 1/8” E7018 electrodes - Cut 2 pieces - ¼” x 2”x 4” mild steel flat bar(use ¼ x 2” Flat bar) - Set amperage setting 90-100 and adjust accordingly. - Set polarity lever to DC only - Set two pieces together at right angles forming a tee joint and tack weld both ends. - Make one bead pass on one side and three overlapping bead passes to complete the fillet weld on opposite side. - Use proper techniques welding in flat position only. - DO NOT TURN IN HOT METAL ## E7018 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Evidence of undercuts 5 pts _______________ Evidence of porosity 4 pts _______________ Evidence of slag inclusion 4 pts ________________ Overlapping techniques 10 pts ________________ Penetration 5 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# LAP WELD – E6011 ONLY #### VERTICAL ONLY #7 PROCEDURE: - Select proper equipment for electric arc welding. - Cut 2 pieces - ¼” x 2”x 4” mild steel flat bar - Select 1/8” E 6011 electrode - Set amperage setting 90-100 and adjust accordingly - Set polarity lever to AC only. - Place the two pieces of metal so they overlap 1 inch. (protect your finished work from spatter.) - Tack weld both ends of plates. - Make a one bead pass on one side and overlapping bead passes to complete the fillet weld on opposite side. - Keep the electrode at an travel angle of 30 to 45 degrees with the lower plate - Hold the arc slightly longer on the lower plate. - Use proper techniques welding in flat position only. - DO NOT TURN IN HOT METAL ## E6011 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 6 pts _______________ Evidence of undercuts 6 pts _______________ Evidence of porosity 5 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 10 pts ________________ Penetration 5 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# LAP WELD – E7018 ONLY #### HORIZONTAL ONLY #8 PROCEDURE: - Select proper equipment for electric arc welding. - Cut 2 pieces -¼” x 2” x 4” mild steel flat bar - Select 1/8” E7018 electrodes - Set amperage setting 90-100 and adjust accordingly. - Set polarity lever to DC only - Place the two pieces of metal so they overlap 1 inch. (protect your finished work from spatter.) - Tack weld both ends of plates. - Make a one bead pass on one side and overlapping bead passes to complete the fillet weld on opposite side. - Keep the electrode at an travel angle of 30 to 45 degrees with the lower plate - Hold the arc slightly longer on the lower plate. - Use proper techniques welding in flat position only. - DO NOT TURN IN HOT METAL ## E7018 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 6 pts _______________ Evidence of undercuts 6 pts _______________ Evidence of porosity 5 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 10 pts ________________ Penetration 5 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# TEE FILET – E6011 ONLY #### VERTICAL ONLY #9 PROCEDURE: - Select proper equipment for electric arc welding. - Cut 2 pieces- ¼” x 2”x 4” mild steel flat bar. - Select 1/8” E 6011 electrode - Set amperage setting 90-100 and adjust accordingly. - Set polarity lever to AC only. - Set two pieces together at right angles forming a tee joint and tack weld both ends. - Make 3 overlapping passes to complete the fillet weld on each side. - Use proper techniques welding in vertical position only. - DO NOT TURN IN HOT METAL ## E6011 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 6 pts _______________ Evidence of undercuts 6 pts _______________ Evidence of porosity 5 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 10 pts ________________ Penetration 5 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# Y-ACETYLENE PUDDLE PAD #10 MATERIALS: - 1 piece of 16 ga. 3”x4” plate steel - #0 or #1 tip, neutral flame, equal oxygen and acetylene pressures. PROCEDURE: - Cut plate steel according to specification. - Plate steel must be off the tabletop. - Place any type of scrap metal beneath the plate. - For welding only, set acetylene & oxygen line pressure gages equal. - Set approximately 4-5 psi on both line pressure gages. - Use a # 0, or #1 tip size - Re-adjust if necessary - Use proper techniques welding in flat position only. - Use a circular or half moon motion to obtain desired width of bead. - Separate each bead approximately ½”. - Make 5 consecutive beads with maximum penetration. - Clean with wire brush and turn in. - DO NOT TURN IN HOT METAL ## PUDDLE PAD Scorecard Follow direction: 4 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Bead appearance 10 pts _______________ Techniques used 5 pts ________________ Penetration 8 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# OXY-ACETYLENE BEAD PAD/ROD #11 MATERIALS: - 1 piece – 16 ga. 3”x4” plate steel - 1/8” bare rod - #1 or #2 welding tip PROCEDURE: - Cut plate steel according to specification. - Plate steel must be off the tabletop. - Place any type of scrap metal beneath the plate. - For welding only, set acetylene & oxygen line pressure gages equal. - Set approximately 4-5 psi on both line pressure gages. - Re-adjust if necessary - Use proper techniques welding in flat position only. - DO NOT TURN IN HOT METAL BEAD /WITH ROD Scorecard Follow direction: 4 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Bead appearance 10 pts _______________ Techniques used 5 pts ________________ Penetration 8 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# OXY-ACETYLENE CORNER WELD #12 MATERIALS: - 2 pieces of 16 ga.1-1/2”x4” plate steel - #0 or #1 tip, neutral flame, equal oxygen and acetylene pressures. PROCEDURE: - Cut plate steel according to specification. - Set the material together tent-like on the welding table - Tack the ends to prevent distortion. - Weld with a semi-circular motion of the torch tip. - Hold tip of inner luminous cone from 1/32 to 1/16 inch from work at 45degree angle. - Set approximately 4-5 psi on both line pressure gages. - Use a # 0, or #1 tip size - Re-adjust if necessary - Use proper oxy-acetylene welding techniques.. - Clean with wire brush and turn in. - DO NOT TURN IN HOT METAL ## CORNER WELD Scorecard Follow direction: 4 pts _______________ Bead width 8 pts _______________ Uniformity of bead 5 pts _______________ Bead appearance 10 pts _______________ Techniques used 5 pts ________________ Penetration 15 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# OXY-ACETYLENE BRAZE WELDING #13 MATERIALS: - 2 pieces – 16ga. x 1-1/2”x4” plate steel - Brazing rod with flux - #0 or #1 tip, neutral flame, equal oxygen and acetylene pressures. PROCEDURE: - Cut plate steel according to specification. - Mechanically clean flat base piece and edges of approximately ½ inch with a grinder. - Make sure pieces fit tightly together. - Preheat total area to 1600 degrees F. or cherry red color. - Apply brazing flux with rod to area where brazing material is to adhere. - Tin weld with thin coating of brazing filler rod. - Build up brazing filler material to proper thickness. - Clean excess flux from weld by buffing or chisel. - DO NOT TURN IN HOT METAL BRAZING LAP WELD Scorecard Follow direction: 4 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Bead appearance 10 pts _______________ Techniques used 5 pts ________________ Penetration 8 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# OXY-ACETYLENE BRAZE WELD ###### PIPE FILLET WELD #14 MATERIALS: - 1 piece of 16 ga x 2”x 2” plate steel - 1 piece of 1-1/2” diameter x 1-1/2” conduit pipe - #0 or #1 tip, neutral flame, equal oxygen and acetylene pressures. PROCEDURE: - Cut plate steel according to specification. - Mechanically clean flat base piece and edges of approximately ½ inch with a grinder. - Make sure pieces fit tightly together. - Preheat total area to 1600 degrees F. or cherry red color. - Apply brazing flux with rod to area where brazing material is to adhere. - Tin weld with thin coating of brazing filler rod. - Build up brazing filler material to proper thickness. - Clean excess flux from weld by buffing or chisel. - Pour water inside conduit pipe to test for water holding capabilities. - DO NOT TURN IN HOT METAL ## PIPE FILLET WELD Scorecard Follow direction: 4 pts _______________ Bead width 5 pts _______________ Uniformity of beads 5 pts _______________ Bead appearance 10 pts _______________ Techniques used 5 pts ________________ Penetration 10 pts ________________ Water holding capabilities 8 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# OXY-ACETYLENE BRAZE WELD LAP JOINT #15 MATERIALS: - 2 pieceS – 16 gax 2”x ” mild steel plate - Brazing rod with flux - #0 or #1 tip, neutral flame, equal oxygen and acetylene pressures. PROCEDURE: - Cut plate steel according to specification. - Mechanically clean flat base piece and edges of approximately ½ inch with a grinder. - Make sure pieces fit tightly together. - Preheat total area to 1600 degrees F. or cherry red color. - Apply brazing flux with rod to area where brazing material is to adhere. - Tin weld with thin coating of brazing filler rod. - Build up brazing filler material to proper thickness. - Clean excess flux from weld by buffing or chisel. - DO NOT TURN IN HOT METAL BRAZING LAP WELD Scorecard Follow direction: 4 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Bead appearance 10 pts _______________ Techniques used 5 pts ________________ Penetration 8 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# OXY-ACETYLENE CUTTING #16 MATERIALS: - 1 piece – 1/4”x 5” steel bar PROCEDURE: - Cut steel bar according to specification, illustrated below. - Measure & mark layout - Use a try square & soapstone to square end. - Use proper procedures in setup & operating oxy-acetylene equipment. - If necessary, use a tip cleaner to clean orifices. - Align the orifices in a manner to permit preheat holes to lead and follow the cut. - Use chart to determine acetylene & oxygen pressures for operation. - Cut marked area. Have instructor check cut area before attempting to make other cuts. - Cut according to specifications. - DO NOT TURN IN HOT METAL ## 2” cuts 5” OXY-ACETYLENE CUTTING SKILL Scorecard Follow direction: 3 pts _________________ Measurements 10 pts __________________ Uniform cuts 10 pts __________________ Visible slag 5 pts _________________ Gouging 6 pts _________________ Proper angle of cut 8 pts ________________ Evidence of beveling 5 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# PLASMA CUTTING #17 MATERIALS: - 1 piece – 3/16”x 5”x ”x 5” steel plate PROCEDURE: - Cut steel bar according to specification, illustrated below. - Measure & mark layout - Use a try square & soapstone to square end. - Use proper procedures in setup & operating plasma cutting equipment. - Clean tip orifices. - Use chart to determine air pressures for cutting operation. - Cut marked area. - Cut according to specifications. - DO NOT TURN IN HOT METAL 1” circle 5” 1” 2” 2” 1” 2” Scorecard Follow direction: 3 pts _________________ Measurements 20 pts __________________ (According to Plan) Uniform cuts 15 pts __________________ Visible slag 10 pts _________________ Safety 2 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – GMAW WELDING

SCORECARD

# BEAD PAD(OVERLAPPING) #### GMAW(GAS METAL ARC WELDING)(MIG) #18 PROCEDURE: - Cut 2 – 3/16” x 2”x 6” plate steel - Select proper voltage according to chart located inside machine. - Set the wire speed according to chart located inside the machine - May need to adjust wire according to sound and welding c. - Re-adjust if necessary - Use proper welding techniques for flat position. - ONE SIDE ONLY – deposit a series of adjacent parallel beads to cover an area 4 x 4 inches. - Each bead must be overlapping ¼ to ½ way with the adjoining bead so that a continuous layer of metal is formed - Chip and clean all slag thoroughly before depositing a second layer - Deposit a second series of parallel beads over the first layer at right angles to the first. - Deposit a third series of parallel beads over the second layer at right angles to the second. - Once completed, clean welds before presenting to instructor. - DO NOT TURN IN HOT METAL ## GMAW ONLY Scorecard Follow direction: 3 pts _______________ Bead width 8 pts _______________ Uniformity of beads 6 pts _______________ Evidence of undercuts 8 pts _______________ Evidence of porosity 4 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 8 pts ________________ Penetration 4 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – GMAW WELDING

SCORECARD

# TEE FILLET #### GMAW(GAS METAL ARC WELDING)(MIG) #19 PROCEDURE: - Cut 2 – 3/16” x 2”x 4” plate steel - Select proper voltage according to chart located inside machine. - Set the wire speed according to chart located inside the machine - May need to adjust wire according to sound and welding c. - Place the two pieces of metal so they overlap ¼ to ½ inch. (protect your finished work from spatter.) - Tack weld both ends of plates. - Use single to cover the lab joint. - Hold the arc slightly longer on the lower plate. - Use proper techniques welding in flat position only. - DO NOT TURN IN HOT METAL ## GMAW ONLY Scorecard Follow direction: 3 pts _______________ Bead width 10 pts _______________ Uniformity of beads 6 pts _______________ Evidence of undercuts 5 pts _______________ Evidence of porosity 5 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 7 pts ________________ Penetration 5 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# Face/Root Stress Test #20 & #21 PROCEDURE: - Select proper equipment for electric arc welding. - Cut 2 - ¼” x 4”x 5” plate steel - Select 1/8” E 6011 electrode - Set amperage setting between 90-100, AC ONLY - Use proper techniques for flat position welding. - Space the metal parts approximately 1/8” apart. - Tack weld both ends to prevent distortion - Position the metal for welding and run a single stringer pass for penetration, tilting the electrode approximately 15 to 30 degrees from vertical in direction of travel. - Upon completion of weld, chip slag and brush the weld clean. - Make two overlapping cover pass for uniformity and quality of weld. - Once completed, clean welds before presenting to instructor. - Use available paint marker to mark your plate specimen. - DO NOT TURN IN HOT METAL Discard discard Cut- Keep keep Cut-- Keep keep cut- ## Keep keep ## cut Discard discard ## 1/8” - Use OA cutting torch or metal shear to cut 1 inch strips for testing. Discard strips as indicate above. - Mark one strip with the letter “F” for face bend (side that has the weld bead) - Mark the other two with the letter “R” for root bend (non-welded side) - Use bench or hand grinder, to grind the welds smooth. - Take strips to weld tester, place the side marked “F” face down on rollers and the plunger on center of weld joint. - Same procedure is used for the root bend. ## E6011 ONLY Scorecard FACE ROOT Follow direction: 10 pts ___________ ___________ Preparation 10 pts ___________ ___________ Evidence of undercuts 5 pts ___________ ___________ Evidence of slag inclusion 5 pts ___________ ___________ Meet stress test 20 pts ___________ ___________ Total 50 pts ___________ ___________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# ELECTRIC ARC WELDING ###### PIPE FILLET WELD #22 MATERIALS: - 1 piece of ¼”x 3”x 3” plate steel - 1 piece of 2” diameter x 2” black pipe - E6011 & or E7018 electrodes PROCEDURE: - Cut plate steel & pipe according to specification. - Place pipe in center of base metal - Use E6011 electrode for a stringer pass - Use E7018 electrode for a cover pass - Check for leaks by pouring water into pipe and let stand - DO NOT TURN IN HOT METAL ## PIPE FILLET WELD Scorecard Follow direction: 4 pts ________________ Bead width 5 pts _________________ Uniformity of bead 5 pts _________________ Bead appearance 10 pts _________________ Techniques used 5 pts ________________ Penetration 7 pts ________________ Water holding capabilities 10 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

Irregularities in Weldment #23 PROCEDURE: - Select proper equipment for electric arc welding. - Cut one piece 1-1/2 X 1-1/2 X 4” angle iron - Set amperage setting accordingly - Set polarity lever to AC only - Re-adjust if necessary - Use proper welding techniques for flat position. - Each bead must be overlapping ¼ to ½ way with the adjoining bead so that a continuous layer of metal is formed - Chip and clean all slag thoroughly before depositing a second layer to prevent slag inclusions. - Deposit enough welds to fill the “V” portion of angle iron - You may cool the specimen in water. - Once cool, use power saw to cut in two pieces (2 inches in length) - Tack weld two piece together to form a “W” - DO NOT TURN IN HOT METAL ## 6011 and/or 7018 Scorecard Follow direction: 5 pts _______________ Bead width 5 pts _______________ Uniformity of beads 5 pts _______________ Evidence of undercuts 5 pts _______________ Evidence of slag inclusion 30 pts ________________ (1 point deduct for each Inclusions) Comment: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept