Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# BEAD PAD – E6011/ 7018 #1 & #2 PROCEDURE: - Select proper equipment for electric arc welding. - Cut one piece ¼” x 5” x 5” mild steel plate - Set amperage setting 90-100 - E6011 Set polarity lever to AC only. E7018 Set polarity to DC - Apply E6011 beads on one- side and E7018 on opposite side - Re-adjust if necessary - Use proper welding techniques for flat position. - Allow ½ “ space from edge of plate to weld bead on all 4 sides. - Each bead must be overlapping ¼ to ½ way with the adjoining bead so that a continuous layer of metal is formed - Chip and clean all slag thoroughly before depositing a second layer - Deposit a second series of parallel beads over the first layer at right angles to the first. - Deposit a third series of parallel beads over the second layer at right angles to the second. - Once completed, clean welds before presenting to instructor. - Other side of plate—use E7018 electrodes (see scorecard) - DO NOT TURN IN HOT METAL ## E6011 ONLY Scorecard E6011 E7018 Follow direction: 2 pts __________ X ____________ Bead width 10 pts ___________ X ____________ Uniformity of beads 10 pts ___________ X ____________ Evidence of undercuts 5 pts ____________ X ____________ Evidence of porosity 5 pts ____________ X ____________ Evidence of slag inclusion 6 pts ____________ X _____________ Overlapping techniques 10 pts ____________ X _____________ Penetration 2 pts ___________ X _____________ Comment: Total 50 pts ____________X ______________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# BEAD PAD – E7018 ONLY #2 PROCEDURE: - Select proper equipment for electric arc welding. - Use the opposite side of the E6011 pad - Set amperage setting 90-100 - Set polarity lever to DC only - Re-adjust if necessary - Use proper welding techniques for flat position. - ONE SIDE ONLY – deposit a series of adjacent parallel beads to cover an area 4 x 4 inches. - Each bead must be overlapping ¼ to ½ way with the adjoining bead so that a continuous layer of metal is formed - Chip and clean all slag thoroughly before depositing a second layer - Deposit a second series of parallel beads over the first layer at right angles to the first. - Deposit a third series of parallel beads over the second layer at right angles to the second. - Once completed, clean welds before presenting to instructor. - Other side of plate—use E6011 electrodes (see scorecard) - DO NOT TURN IN HOT METAL ## E7018 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Evidence of undercuts 5 pts _______________ Evidence of porosity 5 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 10 pts ________________ Penetration 2 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# BUTT WELD – E6011 ONLY #3 PROCEDURE: - Select proper equipment for electric arc welding. - Cut 2 pieces- ¼” x 2”x 4” mild steel flat bar - Select 1/8” E 6011 electrode - Set amperage setting between 90-100, AC ONLY - Use proper techniques for flat position welding. - Space the metal parts approximately 1/8” apart. - Tack weld both ends to prevent distortion - Position the workpiece in flat position, run a single stringer pass for penetration, holding the electrode at a work angle of 90º and a travel angle of 15º to 30º. - Upon completion of weld, chip slag and brush the weld clean. - Make two overlapping cover pass for uniformity and quality of weld. - Once completed, clean welds before presenting to instructor. - Use available paint marker to mark your plate specimen. - DO NOT TURN IN HOT METAL ## 1/8” ## E6011 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 9 pts _______________ Uniformity of beads 9 pts _______________ Evidence of undercuts 8 pts _______________ Evidence of porosity 4 pts _______________ Evidence of slag inclusion 5 pts ________________ Overlapping techniques 5 pts ________________ Penetration 8 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# BUTT WELD – E7018 ONLY #4 PROCEDURE: - Select proper equipment for electric arc welding. - Cut 2 pieces- ¼” x 2” x 4” mild steel flat bar - Select 1/8” E7018 electrodes - Set amperage setting 90-100, set polarity level to positive. - Set polarity lever to DC only - Re-adjust if necessary - Use proper techniques welding in flat position only. - Use a 1/8” gap between plates - Position the workpiece in flat position, run a single stringer pass for penetration, holding the electrode at a work angle of 90º and a travel angle of 15º to 30º. - Complete weld with one overlapping beads, using the weave motion. Make complete weld slightly higher than the level of the plates. - Once completed, clean welds before presenting to instructor. - Use available paint marker to mark your plate specimen - DO NOT TURN IN HOT METAL ## 1/8” ## E7018 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 9 pts _______________ Uniformity of beads 9 pts _______________ Evidence of undercuts 8 pts _______________ Evidence of porosity 4 pts _______________ Evidence of slag inclusion 5 pts ________________ Overlapping techniques 5 pts ________________ Penetration 8 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# LAP WELD – E6011 ONLY #### FLAT ONLY #4 PROCEDURE: - Select proper equipment for electric arc welding. - Cut 2 - ¼” x 2”x 4” mild steel flat bar - Select 1/8” E 6011 electrode - Set amperage setting 90-100 and adjust accordingly - Set polarity lever to AC only. - Place the two pieces of metal so they overlap 1 inch. (protect your finished work from spatter.) - Tack weld both ends of plates. - Make single pass both side to cover the lab joint. - Keep the electrode at an angle of from 30 to 45 degrees with the lower plate - Hold the arc slightly longer on the lower plate. - Use proper techniques welding in flat position only. - DO NOT TURN IN HOT METAL ## E6011 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 8 pts _______________ Evidence of undercuts 8 pts _______________ Evidence of porosity 4 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 8 pts ________________ Penetration 4 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# LAP WELD – E7018 ONLY #### FLAT ONLY #5 PROCEDURE: - Select proper equipment for electric arc welding. - Cut 2 - ¼” x 2”x 4” mild steel flat bar - Select 1/8” E7018 electrodes - Set amperage setting 90-120 and adjust accordingly. - Set polarity lever to DC only - Place the two pieces of metal so they overlap ¼ to ½ inch. (protect your finished work from spatter.) - Tack weld both ends of plates. - Make single pass on both sides to cover the lab joint. - Keep the electrode at an angle of from 30 to 45 degrees with the lower plate - Hold the arc slightly longer on the lower plate. - Use proper techniques welding in flat position only. - DO NOT TURN IN HOT METAL ## E7018 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 8 pts _______________ Evidence of undercuts 8 pts _______________ Evidence of porosity 4 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 8 pts ________________ Penetration 4 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# GMAW #### FLAT POSITION ONLY #9 PROCEDURE: - Select proper equipment for GMAW welding. - Cut 2 pieces - ¼” x 2”x 4” mild steel flat bar - Select proper setting according to thickness of steel product - Set two pieces together at right angles forming a tee joint and tack weld both ends. - Make three passes on one side to complete the fillet weld. - Make a single pass on the opposite side to complete the fillet weld. - Use proper techniques welding in flat position only. - DO NOT TURN IN HOT METAL ## E6011 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Evidence of undercuts 5 pts _______________ Evidence of porosity 4 pts _______________ Evidence of slag inclusion 4 pts ________________ Overlapping techniques 10 pts ________________ Penetration 5 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# TEE FILLET – E7018 ONLY #### FLAT ONLY #8 PROCEDURE: - Select proper equipment for electric arc welding. - Select 1/8” E7018 electrodes - Set amperage setting 90-100 and adjust accordingly. - Set polarity lever to DC only - Set two pieces together at right angles forming a tee joint and tack weld both ends. - Make three passes on each side to complete the fillet weld. - Use proper techniques welding in flat position only. - DO NOT TURN IN HOT METAL ## E7018 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Evidence of undercuts 5 pts _______________ Evidence of porosity 4 pts _______________ Evidence of slag inclusion 4 pts ________________ Overlapping techniques 10 pts ________________ Penetration 5 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# LAP WELD – E6011 ONLY #### HORIZONTAL ONLY #9 PROCEDURE: - Select proper equipment for electric arc welding. - Cut 2 pieces - ¼” x 2”x 4” mild steel flat bar - Select 1/8” E 6011 electrode - Set amperage setting 90-100 and adjust accordingly - Set polarity lever to AC only. - Place the two pieces of metal so they overlap 1 inch. (protect your finished work from spatter.) - Tack weld both ends of plates. - Use single or overlapping welds. - Keep the electrode at an travel angle of 30 to 45 degrees with the lower plate - Hold the arc slightly longer on the lower plate. - Use proper techniques welding in flat position only. - DO NOT TURN IN HOT METAL ## E6011 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 6 pts _______________ Evidence of undercuts 6 pts _______________ Evidence of porosity 5 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 10 pts ________________ Penetration 5 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# LAP WELD – E7018 ONLY #### HORIZONTAL ONLY #10 PROCEDURE: - Select proper equipment for electric arc welding. - Cut 2 pieces -¼” x 2” x 4” mild steel flat bar - Select 1/8” E7018 electrodes - Set amperage setting 90-100 and adjust accordingly. - Set polarity lever to DC only - Place the two pieces of metal so they overlap 1 inch. (protect your finished work from spatter.) - Tack weld both ends of plates. - Use single or overlapping welds. - Keep the electrode at an travel angle of 30 to 45 degrees with the lower plate - Hold the arc slightly longer on the lower plate. - Use proper techniques welding in flat position only. - DO NOT TURN IN HOT METAL ## E7018 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 6 pts _______________ Evidence of undercuts 6 pts _______________ Evidence of porosity 5 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 10 pts ________________ Penetration 5 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# BUTT WELD – E6011 ONLY ##### VERTICAL ONLY #11 PROCEDURE: - Select proper equipment for electric arc welding. - Cut 2 pieces - ¼” x 2”x 4” mild steel flat bar - Select 1/8” E 6011 electrode - Set amperage setting 90-100 - Set polarity lever to AC only - Re-adjust if necessary - Use proper techniquesfor welding in vertical position only. - Use a 1/8” gap between plates - Make a single pass in the bottom of gap. Use a cold back up plate - Complete weld with two overlapping beads or one spread. Make complete weld slightly higher than the level of the plates. - Once completed, clean welds before presenting to instructor. - DO NOT TURN IN HOT METAL ## 1/8” ## E6011 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 6 pts _______________ Evidence of undercuts 5 pts _______________ Evidence of porosity 5 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 6 pts ________________ Penetration 10 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# TEE FILET – E6011 ONLY #### VERTICAL ONLY #12 PROCEDURE: - Select proper equipment for electric arc welding. - Cut 2 pieces- ¼” x 2”x 4” mild steel flat bar. - Select 1/8” E 6011 electrode - Set amperage setting 90-100 and adjust accordingly. - Set polarity lever to AC only. - Set two pieces together at right angles forming a tee joint and tack weld both ends. - Make 3 overlapping passes to complete the fillet weld on each side. - Use proper techniques welding in vertical position only. - DO NOT TURN IN HOT METAL ## E6011 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 6 pts _______________ Evidence of undercuts 6 pts _______________ Evidence of porosity 5 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 10 pts ________________ Penetration 5 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# OXY-ACETYLENE PUDDLE PAD #13 MATERIALS: - 1 piece of 10 ga. 3”x6” plate steel - #0 or #1 tip, neutral flame, equal oxygen and acetylene pressures. PROCEDURE: - Cut plate steel according to specification. - Plate steel must be off the tabletop. - Place any type of scrap metal beneath the plate. - For welding only, set acetylene & oxygen line pressure gages equal. - Set approximately 4-5 psi on both line pressure gages. - Use a # 0, or #1 tip size - Re-adjust if necessary - Use proper techniques welding in flat position only. - Use a circular or half moon motion to obtain desired width of bead. - Separate each bead approximately ½”. - Make 5 consecutive beads with maximum penetration. - Clean with wire brush and turn in. - DO NOT TURN IN HOT METAL ## PUDDLE PAD Scorecard Follow direction: 4 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Bead appearance 10 pts _______________ Techniques used 5 pts ________________ Penetration 8 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# OXY-ACETYLENE BEAD PAD/ROD #14 MATERIALS: - 1 piece – 10 ga. 3”x6” plate steel - 1/8” bare rod - #1 or #2 welding tip PROCEDURE: - Cut plate steel according to specification. - Plate steel must be off the tabletop. - Place any type of scrap metal beneath the plate. - For welding only, set acetylene & oxygen line pressure gages equal. - Set approximately 4-5 psi on both line pressure gages. - Re-adjust if necessary - Use proper techniques welding in flat position only. - DO NOT TURN IN HOT METAL BEAD /WITH ROD Scorecard Follow direction: 4 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Bead appearance 10 pts _______________ Techniques used 5 pts ________________ Penetration 8 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# OXY-ACETYLENE CORNER WELD #15 MATERIALS: - 2 pieces of 10 ga. 2”x4” plate steel - #0 or #1 tip, neutral flame, equal oxygen and acetylene pressures. PROCEDURE: - Cut plate steel according to specification. - Set the material together tent-like on the welding table - Tack the ends to prevent distortion. - Weld with a semi-circular motion of the torch tip. - Hold tip of inner luminous cone from 1/32 to 1/16 inch from work at 45degree angle. - Set approximately 4-5 psi on both line pressure gages. - Use a # 0, or #1 tip size - Re-adjust if necessary - Use proper oxy-acetylene welding techniques.. - Clean with wire brush and turn in. - DO NOT TURN IN HOT METAL ## CORNER WELD Scorecard Follow direction: 4 pts _______________ Bead width 8 pts _______________ Uniformity of bead 5 pts _______________ Bead appearance 10 pts _______________ Techniques used 5 pts ________________ Penetration 15 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# OXY-ACETYLENE BRAZE WELDING #16 MATERIALS: - 2 pieces – 10ga. x 2”x4” plate steel - Brazing rod with flux - #0 or #1 tip, neutral flame, equal oxygen and acetylene pressures. PROCEDURE: - Cut plate steel according to specification. - Mechanically clean flat base piece and edges of approximately ½ inch with a grinder. - Make sure pieces fit tightly together. - Preheat total area to 1600 degrees F. or cherry red color. - Apply brazing flux with rod to area where brazing matherial is to adhere. - Tin weld with thin coating of brazing filler rod. - Build up brazing filler material to proper thickness. - Clean excess flux from weld by buffing or chisel. - DO NOT TURN IN HOT METAL BRAZING LAP WELD Scorecard Follow direction: 4 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Bead appearance 10 pts _______________ Techniques used 5 pts ________________ Penetration 8 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# OXY-ACETYLENE BRAZE WELD ###### PIPE FILLET WELD #17 MATERIALS: - 1 piece of 1/8”x 2”x 2” plate steel - 1 piece of 1-1/2” diameter x 2” conduit pipe - #0 or #1 tip, neutral flame, equal oxygen and acetylene pressures. PROCEDURE: - Cut plate steel according to specification. - Mechanically clean flat base piece and edges of approximately ½ inch with a grinder. - Make sure pieces fit tightly together. - Preheat total area to 1600 degrees F. or cherry red color. - Apply brazing flux with rod to area where brazing material is to adhere. - Tin weld with thin coating of brazing filler rod. - Build up brazing filler material to proper thickness. - Clean excess flux from weld by buffing or chisel. - Pour water inside conduit pipe to test for water holding capabilities. - DO NOT TURN IN HOT METAL ## PIPE FILLET WELD Scorecard Follow direction: 4 pts _______________ Bead width 5 pts _______________ Uniformity of beads 5 pts _______________ Bead appearance 10 pts _______________ Techniques used 5 pts ________________ Penetration 10 pts ________________ Water holding capabilities 8 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# OXY-ACETYLENE BRAZE WELD LAP JOINT #18 MATERIALS: - 2 pieceS – 1/8”x 2”x ” mild steel plate - Brazing rod with flux - #0 or #1 tip, neutral flame, equal oxygen and acetylene pressures. PROCEDURE: - Cut plate steel according to specification. - Mechanically clean flat base piece and edges of approximately ½ inch with a grinder. - Make sure pieces fit tightly together. - Preheat total area to 1600 degrees F. or cherry red color. - Apply brazing flux with rod to area where brazing material is to adhere. - Tin weld with thin coating of brazing filler rod. - Build up brazing filler material to proper thickness. - Clean excess flux from weld by buffing or chisel. - DO NOT TURN IN HOT METAL BRAZING LAP WELD Scorecard Follow direction: 4 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Bead appearance 10 pts _______________ Techniques used 5 pts ________________ Penetration 8 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# ELECTRIC ARC WELDING ###### PIPE FILLET WELD #22 MATERIALS: - 1 piece of ¼”x 3”x 3” plate steel - 1 piece of 2” diameter x 2” black pipe - E6011 & or E7018 electrodes PROCEDURE: - Cut plate steel & pipe according to specification. - Place pipe in center of base metal - Use E6011 electrode for a stringer pass - Use E7018 electrode for a cover pass - Check for leaks by pouring water into pipe and let stand - DO NOT TURN IN HOT METAL ## PIPE FILLET WELD Scorecard Follow direction: 2 pts ________________ Bead width 8 pts _________________ Uniformity of bead 7 pts _________________ Bead appearance 10 pts _________________ Techniques used 5 pts ________________ Penetration 8 pts ________________ Water holding capabilities 10 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# OXY-ACETYLENE CUTTING #19 MATERIALS: - 1 piece – ½”x 3”x ”x 10” steel bar PROCEDURE: - Cut steel bar according to specification, illustrated below. - Measure & mark layout - Cut a 45 degree compound angle - Use a try square & soapstone to square end. - Use proper procedures in setup & operating oxy-acetylene equipment. - If necessary, use a tip cleaner to clean orifices. - Align the orifices in a manner to permit preheat holes to lead and follow the cut. - Use chart to determine acetylene & oxygen pressures for operation. - Cut marked area. Have instructor check cut area before attempting to make other cuts. - Cut according to specifications. - DO NOT TURN IN HOT METAL 1” 1” 1” ## 1” 3” 1 ½” 1 ½ OXY-ACETYLENE CUTTING SKILL Scorecard Follow direction: 3 pts _________________ Measurements 10 pts __________________ Uniform cuts 10 pts __________________ Visible slag 5 pts _________________ Gouging 6 pts _________________ Proper angle of cut 8 pts ________________ Evidence of beveling 5 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# ELECTRIC ARC WELDING ###### PIPE FILLET WELD #20 MATERIALS: - 1 piece of ¼”x 3”x 3” plate steel - 1 piece of 2” diameter x 2” black pipe - E6011 & or E7018 electrodes PROCEDURE: - Cut plate steel & pipe according to specification. - Place pipe in center of base metal - Use E6011 electrode for a stringer pass - Use E7018 electrode for a cover pass - Check for leaks by pouring water into pipe and let stand - DO NOT TURN IN HOT METAL ## PIPE FILLET WELD Scorecard Follow direction: 4 pts ________________ Bead width 5 pts _________________ Uniformity of bead 5 pts _________________ Bead appearance 10 pts _________________ Techniques used 5 pts ________________ Penetration 7 pts ________________ Water holding capabilities 10 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1451 – WELDING

SCORECARD

# PLASMA CUTTING #24 MATERIALS: - 1 piece – 3/16”x 6”x ”x 6” steel plate PROCEDURE: - Cut steel bar according to specification, illustrated below. - Measure & mark layout - Use a try square & soapstone to square end. - Use proper procedures in setup & operating plasma cutting equipment. - Clean tip orifices. - Use chart to determine air pressures for cutting operation. - Cut marked area. - Cut according to specifications. - DO NOT TURN IN HOT METAL ## 45º 1” 3” 3/4” 1” 1” ¼” 6” OXY-ACETYLENE CUTTING SKILL Scorecard Follow direction: 3 pts _________________ Measurements 10 pts __________________ Uniform cuts 10 pts __________________ Visible slag 5 pts _________________ Gouging 6 pts _________________ Proper angle of cut 8 pts ________________ Evidence of beveling 5 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# PLASMA CUTTING #21 MATERIALS: - 1 piece – 3/16”x 6”x ”x 6” steel plate PROCEDURE: - Cut steel bar according to specification, illustrated below. - Measure & mark layout - Use a try square & soapstone to square end. - Use proper procedures in setup & operating plasma cutting equipment. - Clean tip orifices. - Use chart to determine air pressures for cutting operation. - Cut marked area. - Cut according to specifications. - DO NOT TURN IN HOT METAL 2” circle 6” 1-1/2” 2” 2” 2” 2” Scorecard Follow direction: 3 pts _________________ Measurements 20 pts __________________ Uniform cuts 15 pts __________________ Visible slag 10 pts _________________ Safety 2 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – GMAW WELDING

SCORECARD

# LAP WELD #### GMAW(GAS METAL ARC WELDING)(MIG) #22 PROCEDURE: - Cut 2 – 3/16” x 2”x 6” plate steel - Select proper voltage according to chart located inside machine. - Set the wire speed according to chart located inside the machine - May need to adjust wire according to sound and welding c. - Place the two pieces of metal so they overlap 1 inch. (protect your finished work from spatter.) - Tack weld both ends of plates. - Use single to cover the lab joint. - Hold the arc slightly longer on the lower plate. - Use proper techniques welding in flat position only. - DO NOT TURN IN HOT METAL ## GMAW ONLY Scorecard Follow direction: 3 pts _______________ Bead width 8 pts _______________ Uniformity of beads 6 pts _______________ Evidence of undercuts 8 pts _______________ Evidence of porosity 4 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 8 pts ________________ Penetration 4 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – GMAW WELDING

SCORECARD

# TEE FILLET #### GMAW(GAS METAL ARC WELDING)(MIG) #23 PROCEDURE: - Cut 2 – 3/16” x 2”x 6” plate steel - Select proper voltage according to chart located inside machine. - Set the wire speed according to chart located inside the machine - May need to adjust wire according to sound and welding c. - Place the two pieces of metal so they overlap ¼ to ½ inch. (protect your finished work from spatter.) - Tack weld both ends of plates. - Use single to cover the lab joint. - Hold the arc slightly longer on the lower plate. - Use proper techniques welding in flat position only. - DO NOT TURN IN HOT METAL ## GMAW ONLY Scorecard Follow direction: 3 pts _______________ Bead width 10 pts _______________ Uniformity of beads 6 pts _______________ Evidence of undercuts 5 pts _______________ Evidence of porosity 5 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 7 pts ________________ Penetration 5 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# Face/Root Stress Test #24 PROCEDURE: - Select proper equipment for electric arc welding. - Cut 2 - ¼” x 5”x 5” plate steel - Select 1/8” E 6011 electrode - Set amperage setting between 90-100, AC ONLY - Use proper techniques for flat position welding. - Space the metal parts approximately 1/8” apart. - Tack weld both ends to prevent distortion - Position the metal for welding and run a single stringer pass for penetration, tilting the electrode approximately 15 to 30 degrees from vertical in direction of travel. - Upon completion of weld, chip slag and brush the weld clean. - Make two overlapping cover pass for uniformity and quality of weld. - Once completed, clean welds before presenting to instructor. - Use available paint marker to mark your plate specimen. - DO NOT TURN IN HOT METAL Discard discard Cut- Keep keep Cut-- Keep keep cut- ## Keep keep ## cut Discard discard ## 1/8” - Use OA cutting torch or metal shear to cut 1 inch strips for testing. Discard strips as indicate above. - Mark one strip with the letter “F” for face bend (side that has the weld bead) - Mark the other two with the letter “R” for root bend (non-welded side) - Use bench or hand grinder, to grind the welds smooth. - Take strips to weld tester, place the side marked “F” face down on rollers and the plunger on center of weld joint. - Same procedure is used for the root bend. ## E6011 ONLY Scorecard FACE ROOT Follow direction: 10 pts ___________ ___________ Preparation 10 pts ___________ ___________ Evidence of undercuts 5 pts ___________ ___________ Evidence of slag inclusion 5 pts ___________ ___________ Meet stress test 20 pts ___________ ___________ Total 50 pts ___________ ___________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# BUTT WELD – E7018 ONLY #4 PROCEDURE: - Select proper equipment for electric arc welding. - Cut 2 - ¼” x 2” x 4” plate steel - Select 1/8” E7018 electrodes - Set amperage setting 90-100, set polarity level to positive. - Set polarity lever to DC only - Re-adjust if necessary - Use proper techniques welding in flat position only. - Use a 1/8” gap between plates - Make a single pass in the bottom of gap. Use a cold back up plate - Complete weld with two overlapping beads or one spread. Make complete weld slightly higher than the level of the plates. - Once completed, clean welds before presenting to instructor. - Use available paint marker to mark your plate specimen - DO NOT TURN IN HOT METAL ## 1/8” ## E7018 ONLY Scorecard Follow direction: 3 pts _______________ Bead width 8 pts _______________ Uniformity of beads 8 pts _______________ Evidence of undercuts 8 pts _______________ Evidence of porosity 4 pts _______________ Evidence of slag inclusion 5 pts ________________ Overlapping techniques 5 pts ________________ Penetration 7 pts ________________ Safety 2 pts ________________ Total 50 pts ________________

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# ELECTRIC ARC WELDING ###### PIPE FILLET WELD MATERIALS: - 1 piece of ¼”x 3”x 3” plate steel - 1 piece of 2” diameter x 2” black pipe - E6011 & or E7018 electrodes PROCEDURE: - Cut plate steel & pipe according to specification. - Place pipe in center of base metal - Use E6011 electrode for a stringer pass - Use E7018 electrode for a cover pass - Check for leaks by pouring water into pipe and let stand - DO NOT TURN IN HOT METAL ## PIPE FILLET WELD Scorecard Follow direction: 4 pts ________________ Bead width 5 pts _________________ Uniformity of bead 5 pts _________________ Bead appearance 10 pts _________________ Techniques used 5 pts ________________ Penetration 7 pts ________________ Water holding capabilities 10 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

# PLASMA CUTTING MATERIALS: - 1 piece – 3/16”x 6”x ”x 8” steel plate PROCEDURE: - Cut steel bar according to specification, illustrated below. - Measure & mark layout - Cut a 45 degree compound angle - Use a try square & soapstone to square end. - Use proper procedures in setup & operating plasma cutting equipment. - Clean tip orifices. - Use chart to determine air pressures for cutting operation. - Cut marked area. - Cut according to specifications. - DO NOT TURN IN HOT METAL 2” 2” 2” ## 45 2” 3” 2” 2” PLASMA-CUTTING SKILL Scorecard Follow direction: 3 pts _________________ Measurements 20pts __________________ Uniform cuts 10 pts __________________ Visible slag 5 pts _________________ Procedures used 5 pts ________________ Evidence of beveling 5 pts ________________ Safety 2 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

### TOOL CONDITIONING

### SCORECARD

# SHARPENING A TWIST DRILL- FREE HAND Materials needed: - ¼” mild steel rod - Safety glasses - Grinder with adjustable tool rest - Container of water Procedure and Illustration - Using a blacksmith hammer and anvil, flattened one end of the ¼” rod into a shape that resembles a screwdriver. - Use the bench grinder to refine the shape of the screwdriver head so that it will resembles a 12” screwdriver head. - Next, surface grind the length of the screwdriver head eliminating any blemishes, hammer marks, etc. Do not grind across the screwdriver head. - For insure a proper fit, use a # 10 flat head screw provided. ## SCREWDRIVER Scorecard General Shape of head 10 pts ______________ Proper angles 10 pts ______________ Square ness of head 10 pts _______________ Signs of overheating 5 pts _______________ Smooth surface 10 pts _______________ Safety 5 pts _______________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name__________________________________________________

AGSC 1451 – Surveying

Objective:  To establish the length of pace.

Direction:

- You are to pace the measured distance 4 times.

- Record the number of paces for each distance paced.

- Determine the average number of paces

- Calculate the average length of pace.

Part 1:  Determine the average length of pace.

| 100 foot Length | # of paces |
| --- | --- |
| Pace 1 |  |
| Pace 2 |  |
| Pace 3 |  |
| Pace 4 |  |
| Total |  |
| Average Length of Pace |  |

Part 2; Pace the distance between the center of Retama Street to the centered of  Seale Street.  Use your average length of pace to determine the distance.

No of paces: ____________  X Length of pace ________ =  _________________ Distance

Calculate the % error:  _________________

Subtract distance paced from measured distance than divide by measured distance.

Part 3:  Using transit and rod provided, determined the difference in elevation between Point A & Point B? _________________________

| Texas A&M University-Kingsville Agricultural Mechanics Dept. AgSc. 4353- Building Requirements Instructor: Jerome Tymrak | Name(s)_____________________________________ _____________________________________ Date Completed: __________________ |
| --- | --- |

# PLANNING FOR SITE PREPARATION

SKILL SHEET

| Objective: Students will be able to prepare a site for a building by (a) preparing construction site, (b) laying out building lines, (c) setting up batter boards. Directions: - Collect materials and equipment needed - Select site east of AgMech building. - Take given notes in class for added directions. ## Materials needed - 50 to100 foot measuring tape - String or twine - 12- 2”x2”x 2’ lumber - 8- 1”x 4” x 3’ lumber - Double headed nails - Claw hammer - 4-2”x 2”x 8” lumber (corners) - Plumb bob - Sledge hammer Instruction: - Four people per group. - Each group will space their site 5 feet apart. - Each site must be parallel to each other. - Each site measures 10’ wide & 20’ long - Complete the question section of skill sheet. - Have instructor check for set-up & squareness. Questions: Respond to the following in the space provided. - List several considerations in selecting construction site. | - How is the transit level used in construction site preparation? - Explain a method of establishing a 90-degree angle from a building corner stake. - Explain a method of squaring a proposed rectangular or square structure. - Why must a foundation be square? ### Scorecard #### Descriptors; ##### Poss. Pts; Pts Earned. Site Selection; 5. Tools & equipment used; 5. Ability to follow directions; 10. Measurements/squareness; 20. Questions; 5. Safety; 5. ###### Totals; 50. |
| --- | --- |

___________________________________		____________________________                               contestant name			                       school		            chapter #

Direction:  Be sure to print your name, school and chapter ID # in the appropriate places above.  Failure to do so will result in disqualification.

2006 - SOUTH TEXAS INVITATIONAL CDE IN AG MECHANICS

# Plumbing Skill

Introduction:

In this skill you are to calculate, mark and cut plumbing part or items according to the information and diagram given.  You will answer questions over the skill.  You will have approximately 20 minutes to complete this skill.  You may want to refer to the evaluation sheet to see what criteria will be used to evaluate this skill.

Materials needed:

- PVC piping, approximately 12” long

- PVC cleaner

- PVC solvent

- Hacksaw

- Pencil

- Sandpaper

- 2 - 90° elbow

- 1 tee

Procedures and Illustration:

- Measure, mark, cut and assemble PVC piping to fit the diagram below.

| Diagram | Score card |
| --- | --- |
| 10” 5” 5” elbow tee elbow | Outside dimension 20pts _______ Elbows squareness 5 pts _______ “T” centered 10 pts_______ Free from excess glue 5 pts _______ Cleanup 5 pts. _______ Questions 5pts _______ TOTAL 50 pts Note: a deduction of 2 pts for each 1/16” off in measurements. |

Refer to back for questions.

QUESTIONS:

Match the acronym for the each of the following:

___________1.  acrylonitrile butadiene styrene				A.  PVC

___________2.  Polyethylene							B.  ABS

___________3.  Polyvinyl chloride						C.  CPVC

___________4.  Chlorinated polyvinyl chloride					D.  PE

___________5.  Which of the following mentioned above could be used indoors for hot water up to 180°F, provided all controls on the hot-water heater function correctly.

___________________________________		____________________________                               contestant name			                       school		            chapter #

Direction:  Be sure to print your name, school and chapter ID # in the appropriate places above.  Failure to do so will result in disqualification.

2006- SOUTH TEXAS INVITATIONAL CDE IN AG MECHANICS

# Determining and marking a common rafter

Introduction:

In this skill you will calculate and mark a common rafter according to the information given.  You will answer questions over the skill.  You will have approximately 40 minutes to complete this skill.  You may want to refer to the evaluation sheet to see what criteria will be used to evaluate this skill.

Information:

- Safety glasses must be worn during this skill.

- The following materials and supplies are provided at your station.

  - 1” x 4” lumber

  - Framing square

  - Pencil

Procedures and Illustration:

- Assuming you are constructing a small gable-roof poultry house for your show birds, measuring 8 feet wide and 12 feet long with a ¼ pitched roof.  Building is to be constructed on 16-inch centers.

- Add 6 linear inches to the common rafter as an overhang (tail).

- Give the dimensions in feet and inches and fractions of inch to nearest 1/16 inch to the questions on the back.

- You may use the rafter table provided at your station or you may use the rafter table found on the square.

- Determine and mark the 1” x 4” lumber provided according.

| Diagram | Score Card |
| --- | --- |
|  | 1. Rise in inches per foot run? (4 pts) __________ 2. Total rise (A) (4 pts) __________ 3. Length of rafter (B) from upper plumb cut to seat cut? (4 pts) __________ 4. Length of rafter (C) including overhang (tail)? (4 pts) __________ 5. Marking rafter a. upper plumb cut (5 pts) _________ b. length of common rafter (8 pts) __________ c. seat cut (7pts) __________ d. overhang (5pts) __________ 6. Number of rafters needed for building (4pts) __________ 7. Frame ID (5pts) __________ ## TOTAL 50 pts __________ |

___________________________________		____________________________                               contestant name			                       school		            chapter #

# RAFTER QUESTIONS

Direction:  Be sure to print your name, school and chapter ID # in the appropriate places above.  Failure to do so will result in disqualification.  Space is provided for calculation.  Write your answer in the space provided.

### What is the rise in inches per foot run?	 (4pts)						_____________

Answer

What is the total rise in feet, inches and fractions of inch

to nearest 1/16 inch?  (4 pts)								_____________

Answer

### What is the length of rafter (B) ? (see diagram) (4 pts)	                        			_____________

Answer

### What is the length of rafter including the overhang (tail)? (4 pts)			_____________

Answer

### What is the number of rafters needed to complete this project? (4 pts)			_____________

(rafters are placed on 16―inch centers)						                 Answer

See floor model, name the lettered parts related to roof framing. (5 pts)

A. _________________

B. _________________

C. _________________

D. _________________

E. _________________

Name: ____________________________________________

Date Completed: ___________________________________

### TOOL CONDITIONING

### SCORECARD

# SHARPENING A TWIST DRILL- FREE HAND Materials needed: - Dull twist drill - Safety glasses - Angle template or gauge - Grinder with adjustable tool rest - Container of water Procedure and Illustration - Place the drill point against the grinding wheel at approximately a 59-degree angle. - Use one hand near the bit point and wheel; raise the bit cutting point and, at the same time, lower the shank slightly with the other hand during the cutting process. This should form a clearance angle of about 12 degrees. - Use a template to check the proper angle after every stroke. Determine the proper lip clearance by holding the drill bit in a horizontal position and level with the eye. The point or centerline formed by grinding both lips should be 45 degrees to the cutting edge. ## TWIST DRILL Scorecard Cutting lip angles 10 pts _______________ Dead Center angle 10 pts _______________ Heal angle 10 pts _______________ Signs of overheating 5 pts _______________ Smooth surface 5 pts ________________ Length of cuttings 5 pts ________________ Safety 5 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept